## Slide 1: Analysis-Synthesis-Modeling of Inconel 718
An Nguyen

## Slide 2: Overview
A workflow incorporating a series of DREAM.3D, Python, Fortran, MATLAB, and Paraview tools to perform analysis, synthesize statistically equivalent microstructures (SE, and model simulated load on material’s Electron Back-Scattered Diffraction (EBSD).
Included a detailed Read-Me regarding how to operate the workflow.

## Slide 3: DREAM3D Pipeline 1 – Statistical Analysis
Input:
  EBSD file (.ctf, .h5ebsd, and .ang)
Output:
  Stats Generator ODF Angle File (.txt) as input for Pipeline 2
  Pole Figures for Original EBSD (.pdf)
  Feature Data for Original EBSD (.csv) as input for Matlab LognormFit.m
  DREAM.3D Data files (.dream3d and .xdmf) as input to Paraview for visualization of grain microstructure.

## Slide 4: MATLAB Fitting Log-Normal statistic plot on microstructure’s Equivalent Diameter Histogram
Input:
  “Equivalent Diameter” (ED) column from Feature Data of Original EBSD.
Output:
  Log-Normal fit of ED Histogram
  Mu and Sigma values for Pipeline 2

## Slide 5: DREAM3D Pipeline 2 – Microstructure Synthesis
Input:
  Stats Generator ODF Angle File (.txt)
  Mu and Sigma
  Ellipsoidal Ratio B/A and C/A (minor/major length on 2 perpendicular planes)
Output
  Synthetic Statistically Equivalent (SSE) Microstructures.
  Pole Figure for Synthetic EBSD (.pdf)
  Feature Data for Synthetic EBSD (.csv)
  DREAM.3D Data files (.dream3d and .xdmf) as input to Paraview for visualization of grain microstructure.

## Slide 6: DREAM3D Pipeline 3: Abaqus / EVPFFT Input Files
Input:
  DREAM3D file of the Original EBSD (2D) OR
  DREAM3D file of the Synthetic EBSD (3D)
Output:
  Abaqus Hexahedron
  Abaqus FEA Input file
  Abaqus Surface Mesh
OR
  EVPFFT Los Alamos FFT Input file

## Slide 7: EVPFFT
Input:
  EVPFFT Los Alamos FFT Input File
Output:
  Stress and Strain history
  Error/ Convergence history
  Orientation field
  Strain Tensor field
  Stress Tensor field
  Stress gradient
  Orientation Gradient
  VTK files for viewing via Paraview

## Slide 8: Example: Inconel 718 [Grains]
SSE 1
SSE 2
SSE 3
Original

## Slide 9: Example: Inconel 718 [Pole Figures]

## Slide 10: Example: Inconel 718 [EVPFFT on SSEs – S11, S22, S33]
X Load
Y Load
Z Load
SSE 1
SSE 2
SSE 3

## Slide 11: Example: Inconel 718 [EVPFFT on SSEs – Von Mises]
X Load - VM
Y Load - VM
Z Load – VM
SSE 1
SSE 2
SSE 3

## Slide 12: Example: Inconel 718 [EVPFFT on SSEs]
Str_str
Per SSE
Str_str
XYZ Load
Comparison

## Slide 13: Example: Inconel 718 [EVPFFT – Von Mises]